## Slide 1: CONSTRUCTION OF THE WIGGLER DEDICATED TO THE BALDER BEAMLINE OF MAXIV: FROM SOLEIL WIGGLER TO MAXIV WIGGLER
O. Marcouilléa, F. Marteaua,S. Tripathia , A. Thielb, H.Tarawneh b, K. Tavakolia, J. L. Marlatsa, A. Marya, M. Valleaua, J. Vétérana, L. Chapuisa, P. Berteauda, T. El Ajjouria, P. Brunellea, C. Herbeauxa , N. Bechua , A. Lestradea, A. Nadjia , M. E. Coupriea .
aSynchrotron SOLEIL, L’Orme des Merisiers, 91 192 BP 34 Gif-sur-Yvette, France.
bMAX IV Laboratory, Lund University, P.O. Box 118, SE-221 00 Lund, Sweden.
Olivier MARCOUILLE – ESLSXXIV - 28-30 Nov. 2016

## Slide 2: OUTLINE
FEW WORDS ON THE SOLEIL WIGGLER
FROM SOLEIL WIGGLER TO MAXIV WIGGLER: USERS NEEDS AND TECHNICAL CHANGES
MAGNETIC PERFORMANCES
VACUUM LEVEL
CONCLUSIONS

## Slide 3: WIGGLER AT SOLEIL: WSV50
Angular Flux
dF/dW=2.65 1016 E2[GeV] I[A] [Eph/Ec]2 K2/32[Eph/2Ec] Lw[m]/l0
Radiated power
P[kW]=0.633 B2[T] E2[GeV] I[A] Lw[m]
Research of optimum
The radiated power is constant (25 kW)
Scan of the values of (B, Lw)
Evaluation of the angular Flux dF/dW
O. Chubar, NSLSII
P<25 kW
Out-vacuum technology
Problematics
How to produce photons of 50 keV
on an intermediate energy Storage
Ring like SOLEIL (2,75 GeV – 500 mA
and limit the radiated power of a fixed
Length of ID?
50 keV
Critical Energy
Ec[keV]=0.665 B[T].E2[GeV]
Pushing Ec up to 50 keV
BUT Increase of the power
OR….
Increasing the number of poles,
i.e. decrease the period length 
Decrease of the field (B~exp[-ag/l0])
 OPTIMUM of the period Length

## Slide 4: MAGNETIC DESIGN OF WSV50
RADIA Sofware
Cross-check
3 periods model
GIRDERS
Stainless steel 316L
Hyperquench
Vibration
Heat treatment
 Low µ (<1.01)
Technology | Hybrid in-vacuum
Magnets | NdFeB (Br=1.25T/Hc=1950 kA/m) from VAC
Poles | VdPer (Bs=2.35T)
Period length | 50 mm
Number of full periods | 38
Minimum gap | 5,5 mm
Max. magnetic field | 2.1 T
Radiation aperture | +/- 1.8 mrad

## Slide 5: NEEDS AND CONSTRAINTS: MAGNETIC FORCES
Special toolings (magnet mounting)
Stiff girders and powerful motors
Reduce transverse pole size (WSV50)
Force Compensation system
  Magnets (Spring8, SLAC)
  Springs (SOLEIL)
Repulsive
magnet
Magnet
arrays
Carr et al., SLAC
SOLEIL studies (hybrid structure)
Bizen et al., SPRing8
Magnetic gap [mm]
Magnetic force [N]
5.5 mm

## Slide 6: MAGNETIC FORCE COMPENSATION ON WSV50-SOLEIL
Type of spring | Cycle number | Time | Rigidity K [N/mm] | sK [N/mm]
Long | 1 | 170h | 61 | 0.2
Long | 190 | 2h | 62 | 0.3
Short | 1 | 170h | 163 | 0.3
Short | 500 | 5 s | 164 | 0.5
4,5 mm
Spring
Spring Shim
Spring Support

## Slide 7: MAGNETIC FORCE COMPENSATION: EFFECT AND CONTROL
Magnetic system and counter force system
Carriage, magnetic system and Vac. Chamber ends
4,5 mm

## Slide 8: FROM WSV50-SOLEIL TO WSV50-MAXIV: SPECTRAL NEEDS
SOLEIL@2,75 GeV (20 keV50 keV)
MAXIV@3GeV (4 keV40keV)
Aperiodicity (SCW34, CLS)
Tapering of girders (WSV50, MAXIV)
MAXIV predictions
SOLEIL predictions
K=9.8
K=11
MAX: 3 GeV / 500 mA
Construction of a wiggler for the BALDER beamline of MAXIV
Energy range: 4 keV – 40 keV
Collaboration contract signed between SOLEIL and MAXIV in June 2012
Wiggler design inspired from the SOLEIL in-vacuum wiggler WSV50

## Slide 9
E. Wallen, MAXIV
Girders and magnetic system
Tapering of girders
Weak point
K. Tavakoli, SOLEIL
  Operational gap: downto 4.2 mm
  Tapering (2 mm) of girders to smooth the spectrum at low energy (4 keV)
  Pole geometry to increase the field and limit the risk of demagnetization during baking
FROM WSV50-SOLEIL
TO WSV50-MAXIV:
MAJOR CHANGES
Technology | Hybrid in-vacuum
Magnets | NdFeB (Br=1.21T/Hc=2250 kA/m) from NEOREM
Poles | VdPer (Bs=2.35T)
Period length | 50 mm
Number of full periods | 38
Minimum gap | 4.2 mm (taper: 2 mm)
Max. magnetic field | 2.42 T
Radiation aperture | +/- 1.87 mrad

## Slide 10: MAGNETIC DESIGN
Magnetic Field [T]
SOLEIL
Design
MAXIV Design
Good field region
SOLEIL
Good field region
MAXIV
E. Wallen, MAXIV
6 periods model
RADIA Sofware

## Slide 11: ASSEMBLING: PLANEITY CONTROL
3 motors carriage
Stainless steel girders
Laser Tracker
Target
NORTEMECANICA, Spain

## Slide 12: ASSEMBLING: PLANEITY CORRECTION
Amagnetic shims between girders and
Magnet/poles supports
Tuning of spring force with shims
Touch sensor to check: +/-0,03 mm

## Slide 13: MAGNETIC PERFORMANCES: MAGNETIC FIELD
Group3
DANFYSIK
3 mm calibrated Hall probe
Mounted on a mobile carriage
Range: 0 - 3T
Accuracy: 5.10-6 T
Reproducibility:10-5 T

## Slide 14: MAGNETIC PERFORMANCES: FIELD INTEGRALS
HORIZONTAL
VERTICAL
Integrated components vs Gap
Low quadrupolar components
Dipolar components corrected with trim coils
Effect of taper on the field integrals

## Slide 15: INSIDE VACUUM VESSEL ASSEMBLING
Magnetic system displacement
Vacuum vessel mounting
Inside de vacuum vessel
Copper foils
Transition mounting
Extremity flange

## Slide 16: PUMPING AND INSTRUMENTATION
1 500 l/s ion pump
4 150 l/s ion pump
2 NEG Cartridges
2 PENNING GAUGES
15 THERMOCOUPLES

## Slide 17: VACUUM TESTS AT SOLEIL
N. Bechu - SOLEIL
Baking

## Slide 18: DELIVERY AND INSTALLATION IN THE MAXIV TUNNEL
Lifting of 4,7 tons wiggler
Loading before departure to MAXIV
In the MAXIV tunnel
In-situ conditionning:
Gaseous Nitrogen
H.. Tarawneh - MAXIV

## Slide 19: VACUUM TESTS AT MAXIV
M. Grabski/H. Tarawneh - MAXIV
Baking
Baking

## Slide 20: CONCLUSIONS
The Wiggler dedicated for the Balder Beam line is an upgrade version of the wiggler built for SOLEIL
The choice of the technology (PM) results from the need of compacity and zero running costs and maintenance
Major changes and adaptations:
  Functionnal needs
    Tapering of girders
    Operation at low gap
    Magnetic system: geometry of poles
  Specific constraints
    Carriage axis: higher than at SOLEIL
    Measurement bench:
      Adapt the measurement axis
      Measure downto 4 mm
  Control means
    Laser Tracker
    Touch sensor
Wiggler is within specifications in terms of magnetic field level, field integrals, vacuum pressure and is presently ready for commisioning at MAXIV storage ring