## Slide 1: Håkan Rensmo
Electron spectroscopy of solar cell materials
Woodstock 1 2018

## Slide 2: Molecular and Condensed Matter Physics
CMD (UU) Erik Johansson, Gerrit Boschloo, Jesper Jacobson,
KTH Ute Cappel, James Gardner , Lichen Sun, Lars Kloo
SU, Michael Odelius
ÅABC (UU) Kristina Edström, Daniel Brndell,
Cambridge: Sam Stranks
EPFL: - Michael Saliba, Anders Hagfeldt
Bessy: Mihaela Gorgoi, UBjL, Föhlish, Ovsyannikov, Giangrisostomi, Bidermane, Leitner,
Maria Hahlin, Ida Källquist, Dibya Phyal, Bertrand Philippe, Felix Masel, Fredrik Lindgren, Sebastian Svanström,
Former members: Rebecka Lindblad, Susanaa Kaufman.Eriksson
Notes: From fundamental to applied science.
The success of the above is largely linked to an interdiciplinary environment.
In terms of the all aspects of methofdology development.
KOF
Specifically 8 ppeople putting this in the context of energy wit a close colaboration with applied researchers.
Environment for reserchers phd students 50 people.
How o wi bring develop new oportuniteis to energy resech , bring it out to the real applied researchers.
Excelence in developing and using the spectroscopy. And in

## Slide 3: Molecular and Condensed Matter Physics
CMD (UU) Erik Johansson, Gerrit Boschloo, Jesper Jacobson,
KTH Ute Cappel, James Gardner , Lichen Sun, Lars Kloo
SU, Michael Odelius
ÅABC (UU) Kristina Edström, Daniel Brndell,
Cambridge: Sam Stranks
EPFL: - Michael Saliba, Anders Hagfeldt
Bessy: Mihaela Gorgoi, UBjL, Föhlish, Ovsyannikov, Giangrisostomi, Bidermane, Leitner,
Maria Hahlin, Ida Källquist, Dibya Phyal, Bertrand Philippe, Felix Masel, Fredrik Lindgren, Sebastian Svanström,
Former members:
Rebecka Lindblad, Susanaa Kaufman.Eriksson Ute Cappel
HAXPES
Dynamics
Notes: From fundamental to applied science.
The success of the above is largely linked to an interdiciplinary environment.
In terms of the all aspects of methofdology development.
KOF
Specifically 8 ppeople putting this in the context of energy wit a close colaboration with applied researchers.
Environment for reserchers phd students 50 people.
How o wi bring develop new oportuniteis to energy resech , bring it out to the real applied researchers.
Excelence in developing and using the spectroscopy. And in

## Slide 4: X-ray based methodology Our main current development projects
Property | Facility | Technique
TIME RESOLVED | HELIOS (HHG @ UU) | 50 fs, 20-70 eV, time-resolved PES and bandmapping
EFFICIENT DETECTION | UBjL @ Bessy 2 | PES using ArTOF – LowDose-measurements, ps time resolution
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | PES on real buried interfaces during operations. Surface bulk. PDOS.
ENVIRONMENTS II | SPECIES, HIPPIE @ MAX IV | High pressure PES, RIXS on the Li edge
HIGH RESOLUTION | VERITAS @ MAX IV | RIXS > 30 K resolving power
New instruments |  | 
All multi million developments – The energy research very important in the scientific cases
Notes: New opportunities –developed by us may role is to meke design so we can anserr question linked the the energy research
.

## Slide 5: Solar Cell Materials
MODEL
SYSTEMS
REAL
SYSTEMS
COMPLEX
SYSTEMS
Notes: Summarizing second example
We learned that the most efficient dyes have a configuration at the surface were the HOMO level is sticking out from the surface
Facilitate separation and prevent recombination.
This contributed to a new set of dye molecules allowed to a new set of material combination.
Organic I low light intensity application.
Perovskite in flexible and tandem cells
One beeing the perovskite materials inarganic.
The importance of this was then achnoledge in the new familiesof complexes that intern alowed a new generation of redox systems.
With improved properties.
This include the dramatic change removing dye molecules in this consept with perovsket inorganic (or more strictly hybrid) materials
We showed how the photon science could be used to measure how the molecule is oriented at the surface, its energy matching as well as were the electron is how it move from one side into the substrate leaving hole
Realy targeting Real systems.
This concept was then used to design new famillies of dye molecules specifically alowing the change of the electrolyte system and therby hopen for higher voltage systems.
In NREL efficiencicny shart contibuted to this push in efficiencies.
Interestingly in the sam shart there is also the apperence of a different hybrid systems refered to the perovskit solar cells statrin 2013 with values of 10 procent and that has during only a few years reached over 20 procen we have had similar values.
We have olso had an impact on this development using a similar aproch model systems and applied systems

## Slide 6: Electron spectroscopy of solar cell materials
Understand key interfacial processes in conversion
3D design
Electronic structure
Interface structure
Interface structure
Orbital
composition
Where are the atoms?
Energy matching
Where are the electrons?
Dynamics
How do electrons and atoms move during the conversion process.
How to facilitate efficient charge transfer
Goal 1: Explore, at the atomic level, the limitations of conversion due to charge dynamics.
Goal 2: Define design rules for efficient energy conversion. Indoor applications.
Dye
Notes: The over al goal is make more efficient and more stable solarcell
The core of my activity - Understand key interfacial processes …
EXAMPLE 1: Solar energy light excite charges charge separation use in external load.
EXAMPLE 2: Battery external load to move atoms and electrons to new chemistries.
Understand the energetics at the interface. What is the energy of the charges
Understand the organistion of the atoms molecures surfaces to acomplish this.
BOTH SYSTEMS IS UNDERSTANDING CHERG TRANSPORT OVER THE INTERFACE UPON ELECtricgieal (external voltage or photovoltage)
Electronic structure. What is the energy of the electrons that are moving – how do we control the transport
Interface structure - How should the materials/molecules be arranged to accomplish this at interface surfaces.
How the electron store energy by the excitation to different energy levels and how the levels should be designe for charge separation.
How the atoms should be arranged to accopmplsh thus
Solar cells you have a system. Iluminatete you get charge carriers that you have to separate,alow you to tak out the energy in an external load.
Electronic or atomic picture.
Batteries.
Store energy by using a voltage that move charge and creat charged.
In an electon ocr energy level diafram we have move lift and move charges and stor them at different energy levels and thes levels have to match for for directing the process.
Similarly for the battry we move electrons in energy rich electons t and that will bring move the litium ions atoring the energy.
Batteries move Li ions.
Molecular functinal system/solar cell need an arrangment that facilitate the specific process.
-------------------
Methylammonium lead iodide
Hybride material.
Depending on the diffusion length varsus the absortion coefficient.

## Slide 7: Example on atomic level understanding – Light to electrical energy conversion using dye molecules
MODEL
SYSTEMS
REAL
SYSTEMS
COMPLEX
SYSTEMS
Interface structure
Core levels
Example 1
Notes: The battery examples shouwed the methodology development.
An example from light to electrical enery conversion using dye molecules.
The dye- absorbing vissible ligt is the key component in this system and we have invetigatd forst its structure at the surface – interface structure.
By measuring model systems. AUndersting the structure of molecules at.
Based on this Investigate mor COMPLEX systems with dye molecules onnaonostructured surfaces
And then expose these surfeces to liquids we can undesrstand the structure of real/applied interfaces.

## Slide 8: Example on atomic level understanding – Light to electrical energy conversion using dye molecules
Energy matching
MODEL
SYSTEMS
REAL
SYSTEMS
COMPLEX
SYSTEMS
Valence levels
Example 1
Notes: In the sam manner.
Similarly.
Investigating valence levels.
Information about the energy matching.
Simple systems
VBE, HOMO LEVEL and trapstates.
Comparing complex systems Understand how molecular design changes these energy levels,fintuning and finaly aproch realsystems measuring under highe presure with e.g. water understand what happens in real systems.

## Slide 9
+ an undulator giving a lifetime in the storage ring of an hour

## Slide 10
1996

## Slide 11: PES (XPS), Y-axis
Variation of the
photon energy (hν)
Depth of the
analysis
Ekin = hν - Eb
≈ 3 IMFP = f (Ekin)
Soft X-ray: MAX IV
h ν = 50 - 1500 eV
Ekin tunable for each core peak
Hard x-ray: Bessy II
h ν = 2000 – 10,000 eV
Ekin tunable for each core peak
hν
“Universal curve”
In-house XPS
hν=1487 eV
Ekin fixed for each core peak
C1s
Eb=285 eV
Ek = 1202 eV
Ia  ra * sa(hn,q) * exp [-z/L(Ek)]
Property | Facility | Technique
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | PES on real buried interfaces during operations. Surface - bulk. PDOS.
BL51
BLI41
BESSY,
Diamond

## Slide 12: PES (XPS), Y-axis
Ia  ra * sa(hn,q) * exp [-z/L(Ek)]
Property | Facility | Technique
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | PES on real buried interfaces during operations. Surface bulk. PDOS.
Ekin = hν - Eb
hν
BL51
BLI41
BESSY,
Diamond

## Slide 13: Example on atomic level understanding – Light to electrical energy conversion using dye molecules
Orbital
composition
Ligand to Ligand Charge transfer
Long lifetime
HOMO CHARACTER: 2/3 Ru4d +1/3 NCS p
MODEL
SYSTEMS
REAL
SYSTEMS
COMPLEX
SYSTEMS
Example 1
Notes: Used our spectroscopy in a more advance way.
The electron that move around is sometimes refered to as the HOMO
Were is this HOMO electron. The Experimentaly that the HOMO level is distributed at the metalic centar and at the Supher lignands. Sticking out from the surface.
We can do more advanced spectroscopy were we by selection of energies can investigate how particular atoms conmtribut to the valence level or specificvaly the HOMO level which is the lectron with the smallest binding energy, the electron that interact with light in a solar cell and then move around.
For example nitrogen DARK blu atoms her and ruthenium and Ruthenium levels here AND the <lIGHT BLUE. Get
A state with a LONG lifetime
Lonfg lifetiem

## Slide 14: Example on atomic level understanding – Light to electrical energy conversion using dye molecules
Energy matching
MODEL
SYSTEMS
REAL
SYSTEMS
COMPLEX
SYSTEMS
Valence levels
Example 1
Notes: In the sam manner.
Similarly.
Investigating valence levels.
Information about the energy matching.
Simple systems
VBE, HOMO LEVEL and trapstates.
Comparing complex systems Understand how molecular design changes these energy levels,fintuning and finaly aproch realsystems measuring under highe presure with e.g. water understand what happens in real systems.

## Slide 15: Example on atomic level understanding – Light to electrical energy conversion using dye molecules
MODEL
SYSTEMS
REAL
SYSTEMS
COMPLEX
SYSTEMS
Johansson, EMJ et al. Chem. Phys. Chem. 2014,15, 1006 (refs. therein)
Example 1
Notes: Summarizing second example
We learned that the most efficient dyes have a configuration at the surface were the HOMO level is sticking out from the surface
Facilitate separation and prevent recombination.
This contributed to a new set of dye molecules allowed to a new set of material combination.
One beeing the perovskite materials inarganic.
The importance of this was then achnoledge in the new familiesof complexes that intern alowed a new generation of redox systems.
With improved properties.
This include the dramatic change removing dye molecules in this consept with perovsket inorganic (or more strictly hybrid) materials
We showed how the photon science could be used to measure how the molecule is oriented at the surface, its energy matching as well as were the electron is how it move from one side into the substrate leaving hole
Realy targeting Real systems.
This concept was then used to design new famillies of dye molecules specifically alowing the change of the electrolyte system and therby hopen for higher voltage systems.
In NREL efficiencicny shart contibuted to this push in efficiencies.
Interestingly in the sam shart there is also the apperence of a different hybrid systems refered to the perovskit solar cells statrin 2013 with values of 10 procent and that has during only a few years reached over 20 procen we have had similar values.
We have olso had an impact on this development using a similar aproch model systems and applied systems

## Slide 16: Electron spectroscopy of solar cell materials
Understand key interfacial processes in conversion
3D design
Electronic structure
Interface structure
Interface structure
Orbital
composition
Where are the atoms?
Energy matching
Where are the electrons?
Dynamics
How do electrons and atoms move during the conversion process.
How to facilitate efficient charge transfer
Goal 1: Explore, at the atomic level, the limitations of conversion due to charge dynamics.
Goal 2: Define design rules for efficient energy conversion.
Notes: The over al goal is make more efficient and more stable solarcell
The core of my activity - Understand key interfacial processes …
EXAMPLE 1: Solar energy light excite charges charge separation use in external load.
EXAMPLE 2: Battery external load to move atoms and electrons to new chemistries.
Understand the energetics at the interface. What is the energy of the charges
Understand the organistion of the atoms molecures surfaces to acomplish this.
BOTH SYSTEMS IS UNDERSTANDING CHERG TRANSPORT OVER THE INTERFACE UPON ELECtricgieal (external voltage or photovoltage)
Electronic structure. What is the energy of the electrons that are moving – how do we control the transport
Interface structure - How should the materials/molecules be arranged to accomplish this at interface surfaces.
How the electron store energy by the excitation to different energy levels and how the levels should be designe for charge separation.
How the atoms should be arranged to accopmplsh thus
Solar cells you have a system. Iluminatete you get charge carriers that you have to separate,alow you to tak out the energy in an external load.
Electronic or atomic picture.
Batteries.
Store energy by using a voltage that move charge and creat charged.
In an electon ocr energy level diafram we have move lift and move charges and stor them at different energy levels and thes levels have to match for for directing the process.
Similarly for the battry we move electrons in energy rich electons t and that will bring move the litium ions atoring the energy.
Batteries move Li ions.
Molecular functinal system/solar cell need an arrangment that facilitate the specific process.
-------------------
Methylammonium lead iodide
Hybride material.
Depending on the diffusion length varsus the absortion coefficient.

## Slide 17: Synthesis
Figure 6 from Recent progress in efficient hybrid lead halide perovskite solar cells
Jin Cui et al 2015 Sci. Technol. Adv. Mater. 16 036004
doi:10.1088/1468-6996/16/3/036004
Simple: 2 salt solutions, e.g PbI2 + MAI
MA

## Slide 18
FAxMA1-xPb(I1-xBrx)3
MAPbI3
MAPb(I1-xBrx)x
Multi cation (K+, Cs+, MA+, FA+) mixed perovskite
Examples: Lead-based halide perovskite
Time
FA MA
(Also: attempts to replace Pb to Bi, Sn, Sn, Ag)
HAXPES and SOXPES

## Slide 19: TiO2/ CH3NH3PbI3 band alignment
Energy matching
Energy calibrate versus the substrate, i.e. versus TiO2 core level peak (Ti 2p3/2)
see also Philip Schulz et al. Energy Environ. Sci. , 2014.
2010 eV
2.1 eV
VB edge
VB edge
MAPbI3
MAPb(I1-xBrx)x
Notes: Energy level matching
Energy alignment energy calibrated using the substrate signal Ti2p3/2

## Slide 20: XPS gives Partial DOS (not DOS)
Orbital
composition
FA0.85MA0.15Pb(I0.85Br0.15)3
Measurements at high energy mainly measure the PbX6-unit

## Slide 21
Orbital
composition
The top of the valence band has Pb6s - I5p (or Br4p ) anti - bonding character. Defect tolerant.
FA0.85MA0.15Pb(I0.85Br0.15)3
Odelius (Stockholm University)

## Slide 22
Investigation of a mixed perovskie (FA0.85MA0.15Pb(I0.85Br0.15)3)
-10% PbI2
Stoichiometric (0%)
(c) +10% PbI2
Interpretation of the data
Jacobsson et al. JACS 2016, 138, 10331−10343
Theo ≈ 2.55
Interface structure
EXCESS PbI2 FAVOURS PHOTOCURRENT AND EFFIVIENCY
(minimize organic layers that prevent charge transport)
FAxMA1-xPb(I1-xBrx)3
Notes: 2.55 I/Pb is expected
This is in line with the PES-results and points toward a
crystallization process where the perovskite grains are grown
from the outside of PbI2 -grains by diff usion and intercalation of
the organic ions. A surplus of organic ions would facilitate
complete conversion whereas a defi ciency of organic ion may
leave small pockets of unreacted amorphous PbI2 within the
perovskite grains

## Slide 23: efficient luminescence=high PV efficienccy
M. Abdi-Jalebi, et.al , Nature 2018, 555 (7697), 497.
Multi cation (K+, Cs+, MA+, FA+) mixed perovskite

## Slide 24: PES measurements with laser illumination
X-rays and pump laser on same spot on sample
Measure spectra using X-rays
Follow changes induced by laser
Dynamics
Property | Facility | Technique
EFFICIENT DETECTION | UBjL @ Bessy 2 | PES using ArTOF – LowDose-measurements, ps time resolution
515 nm at 1 sun
Mårtensson, Svensson

## Slide 25: Following moving atoms/charges Light induced changes
Property | Facility | Technique
EFFICIENT DETECTION | UBjL @ Bessy 2 | PES using ArTOF – LowDose-measurements, ps time resolution
Dynamics
Pb0
Pb2+
35 min
(FAPbI3 )0.85 (MAPbBr3 )0.15
Notes: For photoinduced measurements, the laser system installed at the
beamline (Tangerine model from the company Amplitude Systemes)
was used at its second harmonic (515 nm), a pulse length of about 350
fs, and a repetition frequency of 208.33 kHz (i.e., 1/6 of the repetition
rate of the synchrotron pulses).
Sample environment
X-FEL (Non linear physics)
and MAXIV
1-10-100 K Wueo developments
Source, detection AND sample environment
KeysTIME AND RESLOUTION FROMSOURCES, EFFICIENT DETECTION AND RESOLUTION FROM THE DETECCTORS.
CLEVER ENVIRONMENT TO MEASURE ON RELEVENT SAMPELS . EVERY THING HAS TO BE DEVELOP.
The building of thes machins is to perform SCIENCE.

## Slide 26: Energy shift, intensity changes and metallic lead
on
off
Time (minutes)
Intensity (normalised)
on
off
Time (minutes)
ΔE (eV)
Time (minutes)
Intensity Pb0 (%)
on
off
(FAPbI3 )0.85 (MAPbBr3 )0.15
Br-
I-
Pb0
e-
e-
h+
h+
Dynamics

## Slide 27: Energy shift, intensity changes and metallic lead
on
off
Time (minutes)
Intensity (normalised)
Dynamics
FAxMA1-xPb(I1-xBrx)3
Multi cation (K+, Cs+, MA+, FA+) mixed perovskite

## Slide 28: Following moving electrons
Property | Facility | Technique
TIME RESOLVED | HELIOS (HHG @ UU) | 50 fs, 20-70 eV, time-resolved PES and bandmapping
How can one control thermalisation ?
Cappel et al. PCCP, 2016, 18 21921-21929
Dynamics
Notes: Sample environment
X-FEL (Non linear physics)
and MAXIV
1-10-100 K Wueo developments
Source, detection AND sample environment
KeysTIME AND RESLOUTION FROMSOURCES, EFFICIENT DETECTION AND RESOLUTION FROM THE DETECCTORS.
CLEVER ENVIRONMENT TO MEASURE ON RELEVENT SAMPELS . EVERY THING HAS TO BE DEVELOP.
The building of thes machins is to perform SCIENCE.

## Slide 29: Time-resolved photoelectron spectroscopy
HOMO
LUMO
Kinetic Energy
Without pump
With pump
Pump
XUV Probe
VIS
Ute Cappel, Johan Söderström, Torsten Leitner et al.
Ovsyannikov, R. et al., J. Electron Spectros. Relat. Phenomena 191, 92–103 (2013)l.
Terschlüsen, J. A. et al., Nucl. Instrum. Methods Phys. Res., Sect. A 768, 84–88 (2014).
.
Dynamics
Notes: To determine the time zero overlap of the probe and pump at the sample and the full width half maximum of the overlap, side bands were measured on helium gas.23 Say that this was only for 800 nm and that FWHM was determined to be 52 fs +- ? here?
39 eV.

## Slide 30: First results
PCPDTBT
Dynamics

## Slide 31
Dynamics

## Slide 32: First results
- 60 fs
0 fs
60 fs
120 fs
270 fs
1000 fs
4000 fs
- 60 fs
0 fs
60 fs
120 fs
270 fs
1000 fs
4000 fs
800 nm
400 nm
Dynamics

## Slide 33: Example on atomic level understanding Next generation – perovskite solar cells
Interface structure
Energy matching
Orbital
composition
Dynamics
Notes: Mother compand is this
Methyl amonium lead Iodied.
Have done similar investigation. Loking simply at the bulk contributions – and then understanding changes in stochiometry in interfacial structures.
Enegy match, learn how to change the controll the absorbtion, coller of the materials and how the energy levels change and in the and match the sunstrat or elekton transporting layer.
Som experimental ide of how the electon look like HOMO beeing an I p antibonding character. Wy this materials is non sensitive to DEFECT STATES.

## Slide 34: Following atoms/charges Voltage induced changes
Property | Facility | Technique
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | Real interfaces during operation
The hard X-ray allow penetration
through the interface
How is the electric field distributed, what is the role of the electrons/atoms.
Example 3
Notes: Thin fiml solar cell configuration
EHL sam shift.
Perovskit has a smaller shift and interestingly the constituents in the perovskit shift differently.

## Slide 35: X-ray based methodology Our main current development projects
Property | Facility | Technique
TIME RESOLVED | HELIOS (HHG @ UU) | 50 fs, 20-70 eV, time-resolved PES and bandmapping
EFFICIENT DETECTION | UBjL @ Bessy 2 | PES using ArTOF – LowDose-measurements, ps time resolution
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | PES on real buried interfaces during operations. Surface bulk. PDOS.
ENVIRONMENTS II | SPECIES, HIPPIE @ MAX IV | High pressure PES, RIXS on the Li edge
HIGH RESOLUTION | VERITAS @ MAX IV | RIXS > 30 K resolving power
(EL.) STRUCTURE | DIFFMAX/HAXPES | Structure and electronic structure in operation
All multi million developments – The energy research very important in the scientific cases
Notes: New opportunities –developed by us may role is to meke design so we can anserr question linked the the energy research
.

## Slide 36
About 50%
Partial DOS of Ru 4d
Ru-complexes a molecular example
Orbital
composition

## Slide 37
Perovskite
VB Character
Orbital
composition
Pb6s-Br4p
Notes: CANNOT SEE Sigma star Pb6s-I5p
MAINLY BR/I P ORBITALS
6 versus 2 electrons
C1s 758 0.077 1487 0.013 8000 ev 0.00008
C2p 0.0022 0.00024 0.00000038
Lead 0.0019 0.00061 0.000035
2.2.2 unit cell DFT DFT Odelius
In our calculation, we have employed
a 2 Å~ 2 Å~ 2 supercell, with approximate dimensions 17 Å~ 17 Å~
25 Å, containing 32 Pb2+ , 96 I− /Br− , and 32 CH3 NH3
+ ions.
The geometries of both the perovskite structures were
optimized i

## Slide 38: Future - Foundation X-ray based methodology Our main current development projects
Property | Facility | Technique
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | PES on real buried interfaces during operations. Surface bulk. PDOS.
Soft 230-800 eV
Hard 2300-18000 eV
Notes: New opportunities –developed by us may role is to meke design so we can anserr question linked the the energy research
.

## Slide 39
Multilayer
Mainly Ru4d
C2p (N,O)‏
Ru-complexes a molecular example
PDOS
Orbital
composition
BL 51, BLI 411 and KMC1/BESSY
Partial DOS of Ru 4d

## Slide 40
hn = 4000 eV
Br3d
I4d
Pb5d
I4d3/2
I4d5/2
+10%
0%
-10%
PbI2
Binding Energy (eV)
Binding Energy (eV)
FAxMA1-xPb(I1-xBrx)3
Use of three energies
i.e.
three analysis depths
Validation of the quantification process with a reference
Jacobsson et al. JACS 2016, 138, 10331−10343
Investigation of a mixed perovskie (FA0.85MA0.15Pb(I0.85Br0.15)3)
-10% PbI2
Stoichiometric (0%)
(c) +10% PbI2
Interface structure
I/Pb ratio of 2.55 is expected
Notes: MOrphology

## Slide 41: X-ray based methodology Our main current development projects
Property | Facility | Technique
TIME RESOLVED | HELIOS (HHG @ UU) | 50 fs, 20-70 eV, time-resolved PES and bandmapping
EFFICIENT DETECTION | UBjL @ Bessy 2 | PES using ArTOF – LowDose-measurements, ps time resolution
ENVIRONMENTS I | HAXPES @ BESSY, SOLEIL, DIAMOND, DESY | PES on real buried interfaces during operations. Surface bulk. PDOS.
ENVIRONMENTS II | SPECIES, HIPPIE @ MAX IV | High pressure PES, RIXS on the Li edge
HIGH RESOLUTION | VERITAS @ MAX IV | RIXS > 30 K resolving power
All multi million developments – The energy research very important in the scientific cases
Notes: New opportunities –developed by us may role is to meke design so we can anserr question linked the the energy research
.

## Slide 42: Electrode-solvent interface
HP-HAXPES at ALS
New feature appearing in O1s spectra due to adsorbed water!
Kaufman-Eriksson et al. Top Catal (2016) 59:583–590 DOI 10.1007/s11244-015-0533-3
BL 9.3.1 ALS (SCIENTA HiPP-2)
Energy matching
4000 eV
Property | Facility | Technique
ENVIRONMENTS II | SPECIES, HIPPIE @ MAX IV | High pressure PES, RIXS on the Li edge
Notes: beamline 9.3.1 of the Advanced Light Source (ALS) at Lawrence Berkeley National Laboratory [30]. The end-station is equipped with a Scienta R4000 HiPP-2 spectromete
HIPPIE upp to 200o eV
Susanna K. Eriksson,† Maria Hahlin,,‡ Stephanus Axnanda,¶ Ethan Crumlin,¶
Regan Wilks,§ Anna I. K. Eriksson,† Zhi Liu,¶ John Åhlund,k Anders Hagfeldt,†
Hans Siegbahn,‡ David E. Starr,§ Marcus Bär,§ and Håkan Rensmo,‡
Department of Chemistry-Ångström, Uppsala University, Box 523, SE-751 20 Uppsala, Sweden,
Department of Physics and Astronomy, Uppsala University, Box 516, SE-751 20 Uppsala,
Sweden, Advanced Light Source Division and Material Science Division, Lawrence Berkeley
National Laboratory, Berkeley, California 94720, U.S.A, Solar Energy Research,
Helmholtz-Zentrum Berlin für Materialien und Energie GmbH (HZB), D-14109 Berlin, Germany,
and VG Scienta AB, Box 15120, SE-750 15 Uppsala, Sweden

## Slide 43: Electrode-solvent interface
S1s
HOMO
0.2 eV shift
0.2 eV shift
Energy matching
Property | Facility | Technique
ENVIRONMENTS II | SPECIES, HIPPIE @ MAX IV | High pressure PES, RIXS on the Li edge
Notes: Mm